DESCRIPTION

FOR INDUSTRIAL USE ONLY. READ PRODUCT DATA & MSDS SHEET CAREFULLY BEFORE USE.

Plow-Slick( is a high-solids clear chemical resistant coating that forms a chemical bond to existing metal and plastic finishes and acts as a final protective shield with phenomenally slick properties

When properly applied and cured, Plow-Slick is more durable than factory applied finishes. Its long pot life (3 - 4 hours depending on temperature and humidity) allows the applicator sufficient open time to hand apply or spray the coating. Plow-Slick can cure at temperatures as low as 38°F or 5°C and at high levels of humidity with proper procedures. Dry times under ideal temperature conditions (70°F or 21°C / 40° Relative Humidity) are 2 hours to touch and a final cure in 48 hours

The coating has been formulated to have the highest gloss (+100 DOI/Delta) offered in protective finishes. Plow-Slick has outstanding abrasion resistance and it’s so durable that just 1 application can generally last an entire plowing season.

Plow-Slick is a high solids (80%), two component low VOC (meets California VOC regulations) inorganic silica/oxygen polymerized hybrid resin system which is “pre-oxidized” making it extremely resistant salt spray, UV rays and abrasion.

Store in a clean, warm area where the temperature remains between 60-90°F or 15-30°C. Cold products are somewhat viscous and will be difficult to mix and apply. Heating of the individual components to 100°F - 30°C prior to mixing may be required to bring the products to the recommended temperatures. This product has a minimum shelf life of one (1) year when stored at 70°F or 20°C in the original sealed container.

# SURFACE PREPARATION

:

Before applying directly to any existing finish or bare metal surface, it is critical to remove wax, release agents, mineral deposits, calcium scale build-up, rust stains, mold, mildew and all other surface contaminants with a pressure washer (3500-PSI HOT WATER recommended) and a commercial degreaser.

After the surface is clean, it must be sanded with 320 grit wet sandpaper and wiped down with lacquer thinner before applying Plow-Slick.

## IMPORTANT

If the surface is not void of contaminants, sanded, thoroughly rinsed and wiped down with lacquer thinner solvent, the coating may not adhere properly.

# APPLICATION-TOOLS

Brushes – short bristle, natural and high density foam brushes; Rollers – short nap (1/4” max.) non-shedding; micro-fiber or high density foam roller covers. Spray Equipment – HVLP, airless or conventional spray system. Nitrile Gloves, Eye Protection, Respirator mask  (if spraying).

Plow-Slick is not very viscous which allows it to be sprayed right after it is mixed. However, if necessary, it may be thinned with xylene solvent up to 5% of the combined Part A and Part B mixed volume.

# MIXING

Mixing ratios are extremely important when blending Plow-Slick. Failure to mix in the correct ratio will result in the coating NEVER drying!  All of the kits shipped will have the correct ratio in each of the 2 containers.

- For the 1-plow kit(s), pour the full contents of each bottle in a clean 5-gallon bucket and mix the two components for 1-2 minutes with a stir stick and then apply.

- For the 1-gallon kit(s), you must use the correct ratios depending on the type of Plow-Slick. Stir Part A for 1-2 minutes before removing any contents. This will assure that all of the pigments are evenly dispersed before you break down into smaller units.

The mixing ratio for the CLEAR - Plow-Slick is 5 Parts (A) to 1 Part (B) by volume.

The mixing ratio for the RED & YELLOW - Plow-Slick is (4) Parts A to (1) Part B by volume.

APPLICATION

Apply with brush, roller or sprayer making sure that you achieve complete coverage. 
A thick coating is NOT needed but a complete coat is!

The coating should be tack-free in approximately 2 hours at 70°F or 20°C and reach a final cure in 48 hours at 70°F or 20°C. Use of xylene will slow down the cure time!

#### CLEAN-UP

Use xylene or lacquer thinner on equipment and a mild citrus soap on hands.

### KEEP OUT OF REACH OF CHILDREN

In case of contact: EYES - Immediately flush with water for at least fifteen (15) minutes. SKIN - Immediately remove from skin with dry cloth followed by thorough washing with a citrus-based soap and water. INHALATION - Remove to fresh air. If breathing is difficult, give oxygen. INDIGESTION - Give large quantity of milk or water, Do not induce vomiting. Contact a physician immediately.

Use only with adequate ventilation when applying indoors. Avoid breathing vapor and spray mist. USE A BREATHING MASK AND PAINTER’S HOOD. Avoid contact with skin and eyes. WEAR FULL LENGTH PANTS AND SHIRTS. Wash hands after using product with a citrus-based soap. Keep all containers closed when not in use.

Do Not Transfer Contents to Un-Labeled Containers and Do not reuse containers. Dispose of all trash in accordance with your local and state laws. Store between 60°F (16ºC) and 90°F (32ºC).

#### ALWAYS USE PROTECTIVE EQUIPMENT
DO NOT TAKE INTERNALLY

# NON WARRANTY

The technical data listed herein has been compiled for your convenience and guidance, and is based upon our experience and knowledge. However, since we have no control over the use of this information of this product, no warranty expressed or implied, is intended or given. EverStone Floors, Inc. assumes no responsibility whatsoever for coverage, performance, or any other damages, including injuries resulting from use or misuse of this information or of products recommended herein.